Admixture Information (AI 6 MBS):

MasterLife® 300 Series Admixtures: DIN 1048 Test Method

The DIN 1048 Part 5 Testing Concrete – Testing of hardened concrete (specimens prepared in mould) is a commonly specified, hydrostatic pressure test method found in project specifications for evaluating the performance of permeability-reducing admixtures.

A summary of this test method is shown below.

DIN 1048 (Hydrostatic Pressure)

Sample - 6 x 12 in. [150 x 305 mm] concrete cylinder

Procedure

- Cast and moist cure the concrete sample for 28 days.

- Cut a 4 in. [102 mm] thick slice from the hardened cylinder.

- Seal the sample sides with aluminum tape.

- Submerge in a water bath for 24 hours.

- Place the sample into the apparatus and apply water pressure.

  - 72.5 psi [0.5 MPa] for 3 days

- Break the sample in half

- Measure the depth of water penetration [in. or mm]

What the DIN Test Measures

Depth of water penetration into the concrete.

Interpretation of Results

- The results are strongly dependent on the conditioning method used which is not specified in the standard.

- This test method can be used to compare the depth of water penetration into concrete consisting of different proportions and/or treatments.